## Slide 1
B4
Single crystal growth of tunable quantum spin systems
Franz Ritter, Cornelius Krellner (Goethe-Universität Frankfurt)
Achievements
Transregional Collaborative Research Centre SFB/TR 49
Frankfurt / Kaiserslautern / Mainz
B2
Introduction
Project goals and work program
Cu-based cyclosilicates: (Ba,Sr)CuSi2O6, BaCu(Si,Ge)2O6 , BaCu(Si,Sn)2O6
Optimization of the growth of large and high-quality single crystals using O2 partial pressure for various substitutions of Sr, Ge, and Sn.
Implementation and optimization of hydrothermal growth for Cu-based cyclosilicates at ~250°C. Y. Chen et al., Dyes and Pigments 105, 167 (2014).
Structural characterisation using pair distribution functional (PDF) analysis of synchrotron data.
Pressure induced stabilization of the tetragonal structure in BaCuSi2O6 at low temperatures (pending synchrotron proposal)
Investigation of the dimensional crossover from 3D to 2D for xSr = 0.1 at Hc1
High field measurements to characterize BEC of substituted systems
B1
S. E. Sebastian et al., Phys. Rev. B 74, 180401(R) (2006):
BaCuSi2O6 single crystal growth using LiBO2 as external flux.
Successful improvement using new flux KBO2 and NaBO2/NaF giving rise to crystals of up to 5 x 5 x 1 mm3 with ~35 mg.
B2
B1
M. Jaime et al., Phys. Rev. Lett. 93, 087203 (2004):
BaCuSi2O6 single crystal growth by the floating zone technique in an O2 atmosphere.
Optimization of the crystal growth for Sr substituted samples, achieved crystal size about 3 x 4 x 1 mm3 with ~18 mg.
Tuning the coupled dimer system BaCuSi2O6
II. Growth from the melt under O2 partial pressure
Crystal growth techniques
Synthesis
I. Flux growth method
Suppression of the structural phase transition with Sr-substitution
a) For x = 0, a first-order phase transition is visible at ~100 K which is suppressed for x = 0.1. b) Susceptibility for two crystals with x = 0 and x = 0.1. The broad maximum shifts to lower T with increasing x, indicating a decrease of the intra-dimer coupling.
This is in agreement with preliminary low-T high-field magnetization data.
Neutron diffraction data for x = 0.1 prove the tetragonal crystal structure with one sort of dimers for x = 0.1. These data were measured at the PSI in collaboration with Christian Rüegg and Denis Sheptyakov. In addition, we will investigate this material in an approved proposal for low-T synchrotron time.
  Requested funding
Research staff: Pascal Puphal (Ph.D. student).
Pascal Puphal will perform crystal growth experiments as well as the structural and physical characterization with the main focus on the Cu-based cyclosilicates and the (Zn1−xGax)Cu3(OH)6Cl2 systems. Furthermore, he will prepare single crystals of the Cs2CuCl4-xBrx series for advanced measurements and perform susceptibility and specific-heat measurements of the other kagome materials.
Small equipment:
    Large bore VSM option for the PPMS, for magnetic characterization of large single crystals (> 4 mm)
    Hydrothermal autoclave for the F-based Kagome systems
    Box furnace for the synthesis of the F-based Kagome systems
Temperature dependent powder x-ray diffraction for x = 0 and x = 0.3 around the structural phase transition. Refined crystal structure at low T is starting point for extended LDA calculations. For x = 0.1, the two leading couplings from the calculations are Jintra and Jinter with Jinter /Jintra = 0.14.
Sr0.1Ba0.9CuSi2O6 crystal growth:
As grown crystals in Pt-boat
Selected single crystal
Laue-diffraction pattern of a single crystal along c
a) Single crystal of BaCuSi2O6 b) Conoscopic image and c) Laue-diffraction reveal the typical layered growth along the crystallographic c-direction
B13N
The Han Purple pigment BaCuSi2O6 reveals a Bose-Einstein condensate (BEC) of triplons above Hc1 = 23.5 T and a dimensional crossover at low temperatures from 3D to 2D at the quantum critical point at Hc1.
M. Jaime et al., Phys. Rev. Lett. 93, 087203 (2004)
S. Sebastian et al., Nature 441, 617 (2006)
The tetragonal crystal structure at room temperature, symmetry group I41/acd s changed below 100 K to the orthorhombic Ibam, leading to two different type of adjacent Cu-dimers in the low-temperature phase.
D. Sheptyakov et al., Phys. Rev. B 86, 014433 (2012)
A3
A5
A7
A8
A9
B1
B2
B5
A12
A10
Studies on BEC:
B13N
a)
b)
c)
a)
b)
c)
x = 0
x = 0.3
H. Berke, Angew. Chem. 114, 2595 (2002):
Various Sr, Ge substitutions sintered at x-dependant temperatures: